TECH SPECS OF ACM,VINYL ,LED ,PET-G & Steel Structure

- LIST OF APPROVED MANUFACTURE ,SUPPLIERS FOR RAW MATERIALS

- Hot Rolled Angles, Channels   - SAIL, VIZAG STEEL, Tata,Jindal.

- M S Plates				         - do-

- CRCA Sheet			       - TATA, SAIL

- GJ Sheet				      -TATA Steel

- Wire Rope				      -Reputed Make

- Stainless Steel Sheet		     -Salem Steel,

- Aluminum Section 		  -Jindal, Agarvansi Or Equivalent Reputed Sources

- Aluminum extrusion		       -	-do-

- Aluminum Sheet		       -Hindalco ,INDAL

- Aluminum composite Material  - Alcoa, Mitsubushi, Alcan, Alucobond ,Alstrong, Alubond, ,Aludecor or As approved by HQ

- PET –G--Spectar-M/s Eastman, VIVAK of M/s Bayer Malilbu Polymers or as approved by HQ

- Polycarbonate Sheet      	-GE Lexena of M/s SABIC, Makrolan of M/s Bayer or as approved by HQ

- Flex					- As Approved by HQ

- Vinyl’s				-Avery,3MAs Approved by HQ

- Tedlar Flim 			-Dupont Or As Approved by HQ

- Primers				-Manufactured Or Reputed

- Paints				- Manufactured Or Reputed

- FRP Matt				- Manufactured Or Reputed

- FRP Resins				- Manufactured Or Reputed

- Fasteners				- Manufactured Or Reputed

- Electrical Wires 			-Reputed Make

- Electrical Protection Devices		-Reputed Make

- Led : CREE/ NICHIA/ OSRAM/ SAMSUNG/ CITIZEN/ PHILIPS (Lumileds)/SEOUL / Epistar

- PET G

Optical Specification

Haze 						ASTM		%	%	<1	<1

D 1003

Light Speculer 					ASTM		%	%	86	86

Transmit ion					D 1003

Diffuse						ASTM		%	%	88	88

Gloss    60 Deg Angel 			            ASTM		Unit	Unit	159	159

Colors, b* CIELBS ILLUMINATES		ASTM		Unit	Unit	<1 	<1

Yellowness CIELAB, Illuminate		ASTM 	Unit 	Unit	<1.5	<1.5

There is no need to pre heat the PET-G materials as in the case of Acrylics and polycarbonate materials.

Finished thermoform piece should be with smooth plane surfaces without dust mark

Dishing, scratches, cracks, Webbing or bridging marks. The Finished part should have consistent gloss.

D.   VINYLS

1. For Screen painting-5 Year Warranty

Design to be printed on 3M or A very make vinyls using automatic and semiautomatic screen painting platform with the inks and clear coat as suggested by Vinyl manufactures. The final graphic displaying vinyl to be aged sealed The opacity of such graphics and vinyl combined on a back lit surface, will carry 5 years warranty for outdoor / indoor application from vinyl supplier only. In order to have combined warranty for vinyl and screen printing from vinyl manufacturer i.e. 3M or Avery, screen printing and printer shall be as per vinyl manufacture advice. These screen printed vinyl will have gasoline resistance property as these are to be fixed in “all the time vapor present area ‘’The warranty, be against print quality failure, color fading adhesioncess and shrinkages, etc. Opaque Vinyl of 3M or Avery with Digital or Screen printing of Graphics as per std design). Letter/Graphics should be cut in such a way that light could pass through the graphics for clear visibility.

These vinyls will be translucent type and will carry a warranty of 5 yrs. For outdoor/indoor application. This warranty will be from manufactures and will be against colour fading, adhesion loss, loss of gloss, shrinkages, Etc

3 STANDERD PROPERTIES

3.1 IS Standards for materials and process to be complied with

Design Condition 			IS 875

Structrual Design and Fabrication 	IS 800

Erection and Installation 		IS 801

Structural Steel 			IS 2062

Hallow Steel Section 			IS 4923

Fastners 				IS 1149

Welding Electodes 			IS 814

Aluminium Sheet			IS 737

Steel Poles 				IS 4923

Structural Steel Work 			IS 226

Bolting					IS 1363

E. INSPECTION AND WARRANT

1. INSPCTION WORK

- BPCL reserved the right to get ACM sample checked and tested by original supplier for its origenal verification.

- Dimantional checks including flatness and levelness will be done after erection of items at RPO. All correlations with code will also be done at RPO.

- If the quantity of material or workmanships is not be libale to pay any compansation for this .

- Vender will submit proof of  materials procurment from approved source.

2 POWDER COATING

wherever powder coating is specified use pure polyster powder for coating after due pretrement paint and powder coation should confirm to

ASTM D-523-60	:	Gloss 60 Deg

ASTM D-5870		:	Cross Hatch Adhesion

ASTM 3363		:	Impact Resistance

ASTM B 117		:	Salt Spray Resistance

ASTM D 2247		:	Humidity Resistance

3 For Pre Treatment

The pre-treatment process is defined as under

- Pre-tretment process sequence for MS Component

Step 1 		- De-greasing

Step 2		-Water Rinse

Step 3		-De-Rusting

Step 4		- Water Rinse

Step 5		-Activation

Step 6		-Zinc Phosphate

Step 7		-Water Rinse

Step 8		-Passivation

Step 9		-Drying

Step 10	-Painting as Specified:

PU Or Powder coated pure polyester.

- Pre –Tretment process for Aluminium Component:

Step 1 		- De-greasing

Step 2		-Water Rinse

Step 3		-Chromiumtizing

Step 4		- Water Rinse

Step 5		-Drying

Step 6		-Passivation

Step 7		- Painting as Specified:

PU Or Powder coated pure polyester.